## Slide 2: CVD of PdZn
Celia Cailloux , 7th of November

## Slide 3: PdZn = Cu
Adding Zn
Zn-CO
Pd-CO
PdZn forms a very stable intermetallic (~ -0.55 eV)
From PdZn form both geometric and electronic effects arise which gives a high degree of tunability with respect to its chemical properties, both activity and selectivity.
For steam reforming of methanol the electronic structure and catalytic effect of the PdZn intermetallic has been shown to resemble that of Cu
Motivation for PdZn

## Slide 4: ”Expected” (desirable) PdZn formation
EXAFS on Pd/ZnO
At 623 K Zn starts to diffuse into the Pd nanoparticles and form PdZn
PdZn layer grows thicker over time
Preferential oxidation of Zn  ZnO segregation and formation of a Pd subshell
For MSR the PdZn is reversible
PdZn
Föttinger, K. (2011). Dynamic structure of a working methanol steam reforming catalyst: In situ quick-EXAFS on Pd/ZnO nanoparticles. Journal of Physical Chemistry Letters, 2(5), 428–433

## Slide 5: APVCD Procedure
Cleaning
Cleaning of ceramics in Aqua Regia
Cleaned the quartz tube in 500 °C ~200 mL/min Ar for 1 h
CVD procedure
Placed the Pd film on top of the ceramic boat with a Zn shot underneath.
Flow Ar (~100 mL/min) for roughly 10 min
Pump down tube
Fill tube with Ar without a flow
Repeat 3 and 4
Reduction & annealing
  Flow 100 mL/min 16 vol.% H₂/Ar and heat to desired annealing temperature for 1 h total
  Flow 100 mL/min 16 vol.% H₂/Ar and heat to desired annealing temperature and leave reducing for 30 min. Then anneal for 1 h total with no flow. Then additional reduction for 30 min.
Cool down in 100 mL/min 16 vol.% H₂/Ar till reaching room temperature
Experimental

## Slide 6: Configurations
Three different configurations
  Placing the Pd film at the end
  Placing the Pd film in the middle
  Changing to a smaller boat  shorter distance between Pd/Si and Zn pellet
Experimental
Flow
A
B
C
Gas
Vacuum pump
Exhaust
Lateral gradient in Pd:Zn
Slow Zn deposition
Lateral gradient in Pd:Zn

## Slide 7: Samples
Gas flow
100 ml/min
16/84 vol% H₂/Ar
Experimental Procedure
Sample | Annealing temperature (° C /K) | Total time at annealing temperature (min) | Annealing time with no flow | Configu-ration
#1 | 600 (873) | 60 | - | A
#2 | 250 (523) | 60 | - | B
#3 | 350 (623) | 60 | - | B
#4 | 350 (623) | 120 | - | B
#5 | 350 (623) | 120 | 60 | C
#6 | 450 (723) | 120 | 60 | C
Flow
A
B
C

## Slide 8: Annealing at different temperatures
ω = 0.5°
Mask = 10 mm
GIXRD

## Slide 9: Annealing at different temperatures - Pd
No pure Pd at T > 523 K
GIXRD - ω = 0.5°, mask = 10 mm
623 K
723 K
873 K

## Slide 10: Annealing at different temperatures
No PdZn
GIXRD - ω = 0.5°, mask = 10 mm
623 K
723 K
873 K

## Slide 11: Annealing at different temperatures
Pd₂Si formation when Zn is no deposited
GIXRD - ω = 0.5°, mask = 10 mm
623 K
723 K
873 K

## Slide 12: Annealing at 873 K  Pd2.352Zn10.648
Flow
Long distance
GIXRD
873 K

## Slide 13: Annealing at 723 K  Pd2.352Zn10.648
No flow
Short distance
GIXRD
723 K

## Slide 14: Annealing at 623 K  Pd₂Si
No flow/flow
Long/short distance
GIXRD
623 K

## Slide 15: Annealing at 623 K  Si on the surface
XPS - survey

## Slide 16: Next steps
Synthesis
Use the large ceramic boat to avoid lateral gradients in the PdZn ratio
Find suitable annealing temperature(s)
Find correlation between temperature and PdZn ratio
Once PdxZny is successfully synthesized
Investigate the thickness of the PdZn and there is a vertical gradient
Investigate zink oxide layer and Pd subshell formation over time
Deposition of alumina (Al₃O₂) and characterize surface
CVD of PdZn

## Slide 17: Any suggestions?
DO CVD at vaiours T for Pd to monitor the PdSi formation